STREAM IST-1999-10341

STREAM Consortium: CNR-LAMEL/ST-MICROELECTRONICS/ /ISEN/SOFT IMAGING SYSTEM/ UNIVERSITY OF SHEFFIELD /IMEC/CNR-IESS/ UNIVERSITY OF PERUGIA

# DELIVERABLE D16

# Work packages nr. 2, Task 2.2 and 2.3

# Partners UniPg, ISEN

# Coordinator ST-Microelectronics

# 3rd report on physical and electrical characterisation of samples for stress measurements

| Main authors: | D. Piccolo, G.Carlotti |
| --- | --- |
| Contributing Author(s): |  |
| Date: | 15 – 08 – 2001 | Doc.No: | IST10341-ST-RP006 |
| Keywords: | STI, STRESS, BRILLOUIN |
| Distribution list: | Mr. B.Netange (EEC), Dr.S.Jones, Dr.H.Cerva Dr. A.Armigliato, Dr. G.Carnevale, Dr. V. Senez, Dr. T. Schilling , Dr. I.de Wolf, Dr. A. G.Cullis, Dr. S. Lagomarsino, Dr. G.Carlotti. |

# Table of contents

Introduction								          p. 3

Process flow and materials for memory cell				          p. 3

Stress characterisation at ST						          p. 5

  - HTO									          p. 7

  - SiON									          p. 7

  - Poly									          p. 8

Elastic characterisation of films by BLS  at UniPg 			          p.13

  - Elastic properties of thermal oxide, high-thermal oxide and

silicon oxynitride films.							          p.14

  - Elastic properties of polysilicon						          p.15

Structures for strain evaluations						          p.17

Conclusion								          p.19

_____________________________________________________________________

# 1. Introduction

Memory cell formation steps can lead to stress generation. In this deliverable main process steps are reported, with details of alternative solutions tested during the third measurement campaign. Test structures designed to evaluate stress phenomena induced by these steps are described.

A complete characterisation of materials used during memory cell formation is reported as well. Parameters for simulations have been extracted.

# 2. Process flow for memory cell

A schematic description of the memory cell flow has been described in section 4 of deliverable D1.

Below it is reported the process flow in details.

| Op. # | Process step | Description |
| --- | --- | --- |
| 1 | STI formation | See D9 |
| 2 | Surface cleaning |  |
| 3 | Tunnel oxide growth | 11 nm |
| 4 | Poly1 layer deposition | 130 nm, in-situ doped |
| 5 | Floating gate definition | Litho + RIE + resist removal |
| 6 | Interpoly dielectric deposition | Oxide – nitride – oxide |
| 7 | Poly2 layer deposition | 25 nm, undoped |
| 8 | Poly2 implantation | P, 4e14 cm-2, 40 keV |
| 9 | Control gate definition | Litho + RIE + resist removal |
| 10 | Source & drain implantation | As, 1.4e15 cm-2, 35 keV, tilt 7° |
| 11 | Thermal treatment (reoxidation) | See after for further details |
| 12 | LDD layer deposition | See after for further details |
| 13 | Spacers definition | RIE |

Tab.1 Gate process flow used to prepare samples.

In the above described process flow, two steps are considered as mainly involved in stress generation:

- memory cell reoxidation: the thermal treatment can induce stress in silicon at the gate edge;

- LDD spacer formation: deposition and RIE definition of a layer can generate stress, due to the direct contact of materials with different thermal expansion coefficient; ion implantation can affect as well stressed regions, inducing defect formation and thus stress relaxation.

For this reason these steps have been further investigated, and different set of samples have been prepared, to study alternative process solutions.

- memory cell reoxidation

Oxidation trials after cell gate definition have been done testing three solutions:

  - standard oxidation (STD): 70Å, 900°C, dry O2, 3h 40’

  - thicker oxidation (REOX1): 100Å, 900°C, dry O2, 5h

  - liner deposition + thermal treatment (REOX2): 100Å

- LDD spacer formation

Different materials have been considered as possible solution for LDD spacers.

As described in deliverable 1, the function of these spacers is to be a mask that protects the region near the gate from subsequent heavy doped source and drain implants. A suitable material for these spacers has to be insulating, to avoid undesired current flows through spacer between gates and between gate and substrate.

Tested materials have been:

  - oxide,

  - nitride,

  - silicon rich oxynitride (SiON)

To obtain the spacer, a film is deposited on patterned wafer and it is then etched by a RIE process. The morphology before and after spacer etch is schematised in fig. 1.

Fig.1  Spacers formation sketch.

For process integration, in the case of a nitride spacer, a thin layer of oxide has to be provided underneath. The aim of this layer is to be a stopping layer during the nitride RIE for spacer definition and to contain stress effect on active area. A subsequent wet etch will remove the remaining thin oxide from silicon surface.

The above-described solutions have been combined, in order to find out the best process.

A123256 lot was devoted to oxidation/ spacer trials. Details of samples are reported in the table below.

| spacers reoxidation | HTO | Nitride | SiON |
| --- | --- | --- | --- |
| STD | #2 | #6 | #5 |
| REOX1 | #9 | #16 | #15 |
| REOX2 | #19 | #24 | #25 |

Tab.2  Patterned samples description.

# 3. Film characterization at ST

For simulation of memory cell definition process, physical parameters of different films are necessary. They are listed below.

  - Undoped polysilicon

  - Doped polysilicon

  - HTO (High Thermal Oxide)

  - Nitride

  - SiON

Nitride had already been characterised during the previous campaigns; as the material is deposited in the same process conditions, it has not been repeated. Samples for the other materials have been prepared.

Mono silicon wafers have been used as a substrate for HTO and SiON film deposition. Polysilicon films have been deposited on a TEOS layer (previously densified), to allow proper measurements by light scattering techniques. For the same reason, film thickness as high as 2500Å or more has been chosen.

Some polysilicon samples have undergone a thermal treatment after deposition, analogous to reoxidation process (STD), in order to obtain a film with properties as close as possible to those of the material of the cell at the end of the process. On these samples a thin layer of oxide is formed, due to the thermal treatment in O2 atmosphere.

The following measurement were carried out in ST:

  - thickness determination by Philips XRF;

  - stress determination by using TENCOR FLX 2400 system. This instrument allowed intrinsic stress measurement but also in-situ stress measurement versus temperature.

These techniques have already been described in the previous deliverable (D12).

A first set of samples (A125724) was sent to UniPG for elastic characterisation. Detailed description of these samples is reported in the table below.

| wf # | Layer | Avg thickness (Å) | Range on wf (Å) |
| --- | --- | --- | --- |
| 1 | HTO | 4494 | 204 |
| 3 | SiON | 4168 | 288 |
| 5 | TEOS + poly (undoped) | 4412 + 2500 | 223 + 15.8 |
| 7 | TEOS + poly (undoped) after reox (+ thermal oxide) | 4438 + 2419 (+ 96.8) | 237 + 15.9 (+ 2.4) |
| 9 | TEOS + poly (doped) | 4400 + 2538 | 228 + 3.0 |
| 11 | TEOS + poly (doped) after reox (+ thermal oxide) | 4431 + 2374 (+ 216) | 229 + 16.8 (+ 7.1) |

Tab.3  Flat samples description (A125724).

It was not possible to measure intrinsic stress and stress vs. temperature for poly on these samples, because a backside removal was needed. Thus a second set of wafers was prepared, analogous to the previous one, just for poly samples. The only difference has been a backside etch of TEOS and poly, prior to stress measurements. Details of samples (A128481) are resumed in tab.4.

| wf # | Layer | Avg thickness (Å) | Range on wf (Å) |
| --- | --- | --- | --- |
| 1 | TEOS + poly (undoped) | 4462 + 2512 | 148 + 12.7 |
| 3 | TEOS + poly (undoped) after reox (+ thermal oxide) | 4494 + 2423 (+ 95.3) | 163 + 15.2 (+ 2.8) |
| 5 | TEOS + poly (doped) | 4394 + 2493 | 164 + 7.9 |
| 7 | TEOS + poly (doped) after reox (+ thermal oxide) | 4492 + 2332 (+ 202) | 159 + 7.6 (+ 8.4) |

Tab.4  Flat samples description (A128481).

### 3.1 HTO film

An HTO film 4500Å thick was deposited on the silicon substrate in a furnace, starting from SiH4.

In ST the sample was measured for precise evaluation of thickness and stress. The results are reported below.

| A125724wf#1: 4500Å HTO on Silicon |
| --- |
| Thickness by XRF | average: 4494Å; range: 204Å |
| Intrinsic stress by curvature measurements | -1.73 109 dyne/cm2 |

Tab.5  Results of ST measurements on HTO.

### 3.2 SiON film

An SiON film 4000Å thick was deposited on the silicon substrate in a PECVD chamber, starting from SiH4 and N2O.

Results of thickness and stress, measured in ST, are reported below.

| A125724wf#1: 4000Å SiON on Silicon |
| --- |
| Thickness by XRF | average: 4168Å; range: 228Å |
| Intrinsic stress by curvature measurements | -8.96 108 dyne/cm2 |

Tab.6  Results of ST measurements on SiON.

### 3.2 Poly film

Polysilicon films have been evaluated both by intrinsic stress measurements at room temperature and by in-situ stress measurement during poly thermal treatment.

The in-situ measurement was performed during a cycle of heating and cooling carried out in a chamber under constant Ar flux, at 8°C/min during the heating step, up to 900°C.

| A128481: 2500Å poly on TEOS |
| --- |
| wf # | poly | Measurements |
| 1 | undoped | Intrinsic, thermal cycle on as dep polysilicon |
| 2 | undoped | Intrinsic |
| 3 | undoped | Intrinsic, as dep and after reox, thermal cycle on reoxidized poly |
| 4 | undoped | Intrinsic, as dep and after reoxidation |
| 5 | doped | Intrinsic, thermal cycle on as dep polysilicon |
| 6 | doped | Intrinsic |
| 7 | doped | Intrinsic, as dep and after reox, thermal cycle on reoxidized poly |
| 8 | doped | Intrinsic, as dep and after reoxidation |

Tab.7   Scheme of poly samples for stress measurements

As these conditions do not reproduce exactly the thermal treatment polysilicon undergoes to during reoxidation, separate stress measurement were performed on amorphous polysilicon (as dep) and on polysilicon after reoxidation.

Both samples of doped and undoped poly were evaluated.

A scheme of the set of samples and performed measurements is reported in tab. 7.

Data of intrinsic stress of poly as dep, and after reoxidation are reported in tab. 8 and 9 respectively.

| A128481: 2500Å poly on TEOS as dep |
| --- |
| wf # | Intrinsic stress by curvature measurements |
| 1 | -4.26 109 dyne/cm2 |
| 2 | -3.28 109 dyne/cm2 |
| 3 | -2.62 109 dyne/cm2 |
| 4 | -2.62 109 dyne/cm2 |
| 5 | -2.62 109 dyne/cm2 |
| 6 | -2.69 109 dyne/cm2 |
| 7 | -2.57 109 dyne/cm2 |
| 8 | -2.83 109 dyne/cm2 |

Tab.8   Results of intrinsic stress measurements on poly as dep.

| A128481: 2500Å poly on TEOS after reoxidation |
| --- |
| wf # | Intrinsic stress by curvature measurements |
| 3 | 1.89 109 dyne/cm2 |
| 4 | 1.85 109 dyne/cm2 |
| 7 | -4.69 108 dyne/cm2 |
| 8 | -6.77 108 dyne/cm2 |

Tab.9  Results of intrinsic stress measurements on poly after reoxidation

The stress profile versus temperature is reported below, for the four tested wafers.

Fig. 2 Stress vs temperature measurements on undoped poly as dep

Fig. 3  Stress vs temperature measurements on doped poly as dep

Fig. 4  Stress vs temperature measurements on undoped poly after reoxidation

Fig. 5  Stress vs temperature measurements on doped poly after reoxidation

The measurements performed on poly as dep show a hysteresis behaviour: a change on poly phase from amorphous to crystalline cause a substantial difference in film stress.

This phase change is confirmed by stress measurement carried out on reoxidised poly. After having undergone the thermal treatment, poly stress in no more affected by heating cycles, showing a nearly linear trend.

# 4. Elastic characterization of films by BLS	(UniPg)

Following the work started during the first period of the project, we have extended the elastic characterization of dielectric silicate glass to thermal oxide, high-thermal oxide and silicon oxynitride films. In addition, preliminary results about the elastic properties of polysilicon have been obtained.  The specimens studied are those listed in the previously presented Tab. 3. In addition, in order to complete the characterisation of silicate glass films reported in previous deliverable D9, we also studied a simple thermal oxide film,  550 nm thick film.

4.1 Elastic properties of thermal oxide, high-thermal oxide and silicon oxynitride films.

The high-thermal oxide (HTO) and oxynitride (SiON) films introduced in Tab. 3, as well as a thermal oxide (TO) film 550 nm thick, have been thoroughly investigated by Brillouin light scattering, in order to achieve a detailed comprehension of the elastic response of these films. As in previous investigations of TEOS and HDP silicate glass films, we have tried to detect as many acoustic modes as possible. In particular, we detected the Rayleigh-Sezawa (R, S1, S2,…) modes, polarized in the sagittal plane. For certain angles of incidence, we could observe the longitudinal resonance (LR) corresponding to a longitudinal wave travelling parallel to the free surface. Finally, in the case of TO and HTO films, we could also reveal the longitudinal bulk mode (LB), travelling at an angle with respect to the film normal, as shown in Fig. 6.

Fig.6.  Brillouin spectra relative to the HTO and SiON films. The angle of incidence is 70°.

| Material | H (nm) | ( (Kgm-3) | C11 (GPa) | C44 (GPa) | E (GPa) | ( |
| --- | --- | --- | --- | --- | --- | --- |
| Thermal oxyde | 550(20 | 2350(50 | 79.6(2 | 30.4(1 | 72(3 | 0.19 (0.02 |
| HTO | 450 | 2200 | 79.5 | 31.0 | 73 | 0.18 |
| SiON | 417 | 2150 | 97 | 34 | 84 | 0.23 |

Tab. 10 Mass density and elastic parameters of the films investigated

In order to extract the elastic constants values, the information about the mass density of each film  was obtained from x-ray reflectivity measurements performed at the Physics Dept. of the University of L’Aquila. This permitted us to achieve a complete elastic characterization of the films studied. The obtained results are reported in Tab. 10. As a general comment to the results obtained we can say that the hypothesis of isotropic elastic media has been verified for all the specimens. The obtained elastic constants of TO and HTO are quite similar to those of HDP films. Concerning SiON, although a rather low value of the mass density was measured, probably due to residual hydrogen inclusion during deposition, the presence of nitrogen causes a marked hardening of the film with respect to oxides. In particular the Young’s modulus is about 15% higher than in the case of oxides.

## 4.2 Elastic properties of polysilicon

Brillouin scattering measurements has been also performed on the double layer structure consisting of a TEOS (about 440 nm) and a Polysilicon (about 250 nm) film grown on Si wafer (#5 in Tab. 3). This is a very interesting inhomogeneous medium for acoustic propagation, because one has a ‘soft’ (TEOS) film embedded between two harder materials (Si and polySi). Different acoustic modes have been observed in the spectra, as shown in Fig. 7. The experimental evidence we have obtained from our measurements is that the elastic constants of polySi does not depend on the doped or undoped condition. In fact, we obtained exactly the same values of the phase velocities in either undoped or doped samples, within the experimental uncertainty of about 1%. In addition, we could estimate the elastic constants of polySi, assuming those of TEOS to be known from previous investigations (see deliverable D9). Our polySi films, as shown in Tab 11, are softer than expected on the basis of one of the most recent result, from W. Sharpe’s group at John Hopkins University. However, in the same paper of the Sharpe’s group,  results about the Young’s modulus of polySi from other groups are reported. These values are rather scattered in the interval 137-173 GPa. This means that our results indicate a value of E at the bottom of the range of values found in previous investigations using different methods.

Fig .7  Comparison between the calculated dispersion curves of the phase velocities of the different acoustic modes of the polySi/TEOS/Si heterostructure investigated and the measured velocities (triangles). Solid curves are the best fit ones, while dashed curves are calculated using the constants of polySi reported in the literature.

|  | C11 (GPa) | C44 (GPa) | E (GPa) |  |
| --- | --- | --- | --- | --- |
| Literature* | 192 | 69 | 169(6 | 0.22(0.1 |
| This work | 162(8 | 55(2 | 137(6 | 0.24(0.3 |

*W.N.Sharpe and K. Jackson, to appear in the Proceedings of the SEM 2000

Tab. 11  Elastic constants of polysilicon

# 5. Structures for strain characterization of cell array

Besides microsections, already described in deliverable D9, the test pattern ZZ64 offers some structures for cell array stress characterisation. They are generally indicated as ‘cast’ and propose different combinations of isolation features and poly length.

Their position in test pattern is reported in Fig. 8.

Fig. 8. Test pattern lay-out with microsection and cast position

Fig. 9.  Cast detail

Fig. 9 shows a detail of cast area.

Different casts are related to by a number from 1 to 11. A description of dimensions involved in each cast is reported in Tab 12.

| Cast # | Active area width (µm) | Active space (µm) | Poly length (µm) |
| --- | --- | --- | --- |
| 1 | 0.16 | 0.32 | 0.26 |
| 2 | 0.16 | 0.32 | 0.26 |
| 3 | 0.16 | 0.32 | 0.26 |
| 4 | 0.16 | 0.32 | 0.26 |
| 5 | 0.16 | 0.32 | 0.52 |
| 6 | 0.16 | 0.32 | 1 |
| 7 | 0.52 | 0.32 | 0.26 |
| 8 | 1 | 0.32 | 0.26 |
| 9 | 5 | 5 | 0.26 |
| 10 | 0.16 | 0.32 | 2 |
| 11 | 0.16 | 0.32 | 5 |

Tab. 12.  Cast description

These casts allow the evaluation of stress as a function of cell array dimensions. Typical dimensions for a 0.15 µm technology are considered: 0.16 µm active area, 0.32 µm space and 0.26 µm poly length. Thus casts from 1 to 4 are representative of a typical cell array. In fig. 10 a top view of a single memory cell is reported. Wcell refers to active area width, and Lcell to poly length.

Fig. 10. Cell lay-out.

# 6. Conclusion

A set of morphological samples has been prepared to evaluate stress involved in memory cell formation. Patterned wafers will allow measurements by CBED technique and (-Raman. In order to determine parameters needed for simulations, flat wafers of films involved in this process module have been prepared and tested: elastic characterisation has been carried out and data are now available.

# Footnotes

W.N.Sharpe and K. Jackson, to appear in the Proceedings of the SEM 2000